## Slide 1: Fig. 8
1 m
A
B
C
D
Notes: XRF-STXM-details.pdf 10 Feb 2013 - elastic scatter (angle) never published
A – insert) Image: 100628033 (1700 EV, circle is known as hot spot
A) Polarization dependence : XGLabd (txt) 100628012.dta to 100628019.dta (20 is 300 sec also at 1700 eV
B) from excel file: XRF-elastic-signal-Jun2010.xls
C) Envi_Sci_Tech (2012) Fig. 3B
D) Envi_Sci_Tech (2012) Fig. 3C

## Slide 2: Fig. 9
Fe map bio map (pre-Fe)
2 um
As Fe As/Fe
500 nm
Arsenic
64
0
Iron
136
0
a
b
c
d
e
Notes: From SXM-London-2012.ppt WHAT IS PUBLISHED ?
(b) Stxm11\2010\10-10\10-02\001 Y:\data\XRM\stxm-11\2010\10-10\10-02
(a) XRM\stxm-11\2010\10-10\10-02\003 stack of stacks (bit integrated XRF)
(c-d) ???

## Slide 3: Optimized fit
As(III) non-As As(V)
As(III)
70
-5
As(V)
non-As (constant)
As-V
As-III
130
-5
12
05
OD / um
Residual
absolute
mask
As(III) 34
As(V) 88
const 6.8
V/III 2.6
As(III) 50
As(V) 58
const 6.7
V/III 1.2

## Slide 4: As-XRF-mapping - ref
Mg signal from XRF yield
Likely composition ? MgO ?
XRF-yield NEXAFS
OD1
Mg
As-3
As-5
As(V) scorodite
As(III) tooeilite
MgO (from XRF?)
As(III) non-As As(V)
As(III) tooeilite
As(V) scorodite
Digitized ref. spectra from
Geochim_Cosmochim_Acta
72_2008_3949-As-NEXAFS-acid-mines.pdf
Notes: Digitized ref. spectra from Geochim_Cosmochim_Acta_72_2008_3949-As-NEXAFS-acid-mines.pdf
As XRF-yield NEXAFS: stxm11\2010\10-10\10-03\03-02\003 Y:\data\XRM\stxm-11\2010\10-10\10-02\11_101002003

## Slide 5: As-XRF-mapping – fits(1)
As(III) non-As As(V)
As(III) tooeilite
As(V) scorodite
As(III)
44
0
75
0
As(V)
non-As (constant)
As(III) 14
As(V) 36
const 5.4
As(III) 18
As(V) 20
const 4.4
As(III) - rich
As(V) - rich
Extend range to 1380 eV & Smoothing ref. spectra will improve fits
As(III) tooeilite
As(V) scorodite
III-rich & V-rich pectra differ !

## Slide 6: As-XRF-mapping – fits(2)
As(III) tooeilite
As(V) scorodite
As(III) 24
As(V) 58
const 5
As(III) 29
As(V) 33
const 4
As(III) - rich
As(V) - rich
Extend range to 1380 eV & Smoothing ref. spectra will improve fits
As(III) tooeilite
As(V) scorodite
III-rich & V-rich spectra differ !
Improve ref.
OLD FIT
XRF-yield red spectra

## Slide 7: CLS_Feb2012_Mg_As_maps
Example of use of stacks~analyse~XRF-stack-of-stacks
2 um
A
C
All peak
Mg
As
As Mg “bio”
As signal
Mg signal
44 OD (1300 eV)
Clipped 0.8
8
0
nm
2 um
As
Mg
B
1.2
0
Notes: CLS Feb 2012 stack A120205008 (*.ssb – all XRF saved) stack stack A120205046 – channels only (but Mg / As )
A) A120205044 area for stack 46 (lower slits & flux; PMT, 1 ms dwell