TUTORIALS to illustrate use of aXis2000

For the analysis of STXM *.sdf data

File: aXis2000-tutorials.doc

Author: Adam Hitchcock

Last changed:  11-Jan 2023

CONTENTS

A. Image manipulation

A.1. Reading a 532stxm image

A.2. Converting  transmission  to optical density (OD)

A.3. Determining profiles across an image

A.4. Removing noise from images

A.4.1 Replacing lines

A.4.2 Smoothing images

A.4.3 Fourier filtering images

A.4.4 Clipping  images

A.5 displaying multiple  mages

B Spectral Manipulation

B.1 Reading in a spectrum

B.1.1 Reading stxm5.3.2 multiple region spectra

B.1.2 Reading stxm7.0.1 spectra

B.2 displaying multiple  spectra

C. Linescan processing

C.1 Reading in and preparing linescan in OD

C.2 Extracting and comparing spectra

C.3 Fitting linespectra

D. Stack processing

D.1 Read als5.3.2.2 stack & convert to OD

D.2 Extract reference spectra from the *od stack

D.3 Creating chemical maps from SVD fits

-------------

# A. Image manipulation

## A.1. Reading an ALS 532stxm image

* start  aXis2000

* Read~STXM (sdf)

Browse	- select   ~\sdf-image.hdr

OK

Notes: The image is a 30x30 micron image of a wet cross-linked gel recorded at 396 eV. The upper right portion of the image is off-the-edge of the gel, passing through 2 silicon nitride windows and about 1 micron of water.  (20320063)

## A.2. Converting  transmission  to optical density (OD)

[read in sdf-image.hdf]   - tutorial #A.1.

* determine average signal in ‘white’ area (no sample) by either

* move mouse over ‘white area’, read value from the cursor

-or-

* Images~Average pixels~region- all pixels

You should find a value of about 4500.

* Images~Convert_to_OD

* type 4500

The OD image is computed (OD = ln(4500/image); it is placed in buffer #0 – the default temporary buffer.

* Copy Buffer, click on any empty thumbnail to copy the image to a permanent buffer.

## A.3. Determining profiles across an image

[read in sdf-image.hdf]   - tutorial #A.1.

[convert to OD] – tutorial #A.2.

*Images~profiles~linear

- click at start of line, move mouse to end of line and click again

- select a buffer to store profile in; provide name if desired

- the OD intensity along the line is displayed

## A.4. Removing noise from images

### A.4.1 Replacing lines

[read in sdf-image-noisy.hdf]   - tutorial #1

* Images~Replace line~manual-H

- move cursor to just above the lower black horizontal line.

The x, and y line number (lower left panel)  should be 11

- click mouse.

Line 11 is replaced by average of line 10and line 12,  and the result is moved to buffer #0.

* Images~Replace line~manual-H

- click on the upper part of the dark upper line – you will probably identify line 138.

- select ‘no’ then take the default in the next interaction box. Which will replace line 138 with lone 139.

- repeat to replace line 137 with average of lines 136 and 139.

Note in this case, using the default (average adjacent lines) would leave a distortion in the image since two adjacent corrupt lines make up the upper dark line

### A.4.2 Smoothing images

[read in image-to_smooth.axb using Read~images~axis]

* Filter~smooth

3- or 5-point smoothing reveals details of this image better.

### A.4.3 Fourier filtering images

[read in image-to_clean.axb using Read~images~axis]

* Filter~clean (FT image filter)

use cursor in rubber band mode (click at start, release, drag to end, click and release) to draw a rectangle top to bottom around the vertical line to the left of the central spot.

NB 2D Fourier transforms ech quadrant is a replica of the other 3, so filtering out a pattern in one quadrant is all that is needed

This is an image of a toner particle. The moiré pattern arises from beating of the frequency of  vibrations of  beamline optical element(s) against the ~kHz acquisition frequency.

### A.4.4 Clipping  images

[read in image-to_clip.axb using Read~images~axis]

* Images~clip signal~histogram

- a histogram of the z-values of this signal will appear. Select lower and upper bounds of data to be retained by moving mouse to lower limit of physically meaningful  data (-15), click, then to upper limit (280), click.

- the pixels with values below the lower and above the upper limit are set to the closest limit and the result is placed in buffer #0.

* Copy buffer to move the result into a permanent buffer

This is the  map of styrene-co-acrylonitrile  (SAN) from a fit a C 1s image sequence of a filled polyurethane. The haze is removed because pixels with large negative values are removed. These negative values from a fit are likely  because the reference spectra are slightly wrong. clip signal~histogram removes these artificial results revealing more clearly the spatial  distribution of the SAN particles.

## A.5 displaying multiple  Images

* Read~images~axis  image-to_clean.axb into buffer # 1

* Fourier filter this image to remove moiré noise (see Tutorial #A.4.4)

* Copy buffer to move the result into buffer # 2

* Add~buffer #1 with -1 weighting to buffer #2

* Copy buffer to move the difference (removed noise)  into buffer # 3

* view buffer # 1 by clicking on thumbnail #1

* Filter~smooth (3-point) the data; move to buffer #4

* Display~thumbnails~4~common scale  selecting  [1,2,3,4)

This type of comparison can help decide optimum processing. Note that the lineouts are active and give quantitative signal levels of all 4 displayed signals.

# B Spectral Manipulation

## B.1 Reading in a spectrum

### B.1.1 Reading stxm5.3.2 multiple region spectra

- start in buffer #1

* read~STXM (sdf) browse to select 11103106.hdr

- in Region pull down menu, scroll to bottom, select all regions; OK

Seven  spectra will be read. Convert spectra in buffers 1 -6  to OD by:

- select buffer #1  Specrtra~Convert to~OD;  buffer 7 (Io)

- transfer result to buffer#1

*  - select buffer #2 , 3, ,4,  #5 (mtx), buffer #3 (pipa), #2 (san) and convert to OD using buffer #7 as Io. After generating each spectrum, transfer it to a suitable buffer to store for later spectral comparison

This is a set of 7 point spectra acquired at same time on a 355 filler polyurethane sample. region 1: pipa (missed); 2, 6 - SAN, 3 - pipa;, 4 - edge of SAN, 5 - matrix, 7, hole. (Stacks measured on this type of sample are used in the Advanced tutorial).

The points at which these spectra were obtained can be viewed by:

* read~images~graphics~png~image 355-point-spectra.png

images recorded before and after these point spectra:

11103104 (285 eV) - highlights SAN, PIPA

11103105 (287 eV) - only SAN

11103107 (289 eV) - convert to OD; use Z-scale to check for damage

11103108 (285 eV) - should be same as 104

# C. Linescan Spectra processing

## C.1  READ, Display, convert to OD

1. Read~STXM (sdf) stxm532-linescan

2. extract Io (in region without sample)

Linescans~Add lines~horizontal  (y-valeus 1.0 – 1.5);

Store in a permanent buffer (e.g. 6)

3. convert to OD, Linescans~normalize to Io  buffer 6

## C.2 Extracting and comparing spectra

4. Read~Images~axis  355-linescan-od.axb

(This has already been converted to OD using the lower part of the line, off the polymer sample; it is the same sample as in D)

5.use linescans~Add lines~horizontal to  extract the

matrix (8.7 – 10.0) , pipa (11.8-12.0) and SAN (13.3-14.00 spectra (numbers are position along the line)

6. write each of these spectra to disk  (Write~axis, and put name of the chemical species at start of header)

### C.3 Fitting linescan spectra

# 7.   Linescans~linefit 355-linescan-od.axb, the 3 components, select matrix, then pipa, then SAN spectra written our in step 6. Store the parameter file - 355linescan_matrix_pipa_SAN.par

# 8. Spectra are plotted in buffers 1,2 , 3, which the distribution along the line for matrix, pipa and SAN are displated in buffers 4, 5, 6. The residual of the fit is stored to disk (355-linescan-OD_3SVD_res.axb).

# D. STACK processing

#### D.1 Read als5.3.2.2 stack & convert to OD

532_010817014  is a 38 energy C 1s stack  measured on a polyurethane polymer consisting of 2 types of aromatic particles (SAN and pipa) in an aliphatic matrix [Ultramicroscopy 88 (2001) 33]

- Convert STXM-sdf stack to an aXis2000  file

- Read~STXM (sdf) \532_010817014\10817014.hdr

region#1 polymer     region#2  - Io off microtomed section

– output is  *.ncb,*.dat’, where * is  user selected name.

the saved stack is then opened in Stacks~Analyze~stack_process

- Align if needed (but this stack did not need alignment)

- After reading region 2, select i: All and save the Io file

- Stacks~Analyze~stack_process *.ncb. Read Io from file; convert to OD; write out the stack *od.(ncb, *,dat)

#### D.2 Extract reference spectra from the *od stack

5.	Stacks~Analyze~stack_process *od.ncb

6.	 Play back stack as a movie, Select I-region of largest particle. 	You should see a spectrum with 2 strong peaks, one at 285.1 eV  	(*(C=C)) the other at 286.6 eV (*(CN)) save as *-SAN

7. 	click on the spectrum display a the 286.6 eV peak. Some of the particles should disappear – they are the PIPA particles. Go back to 285.1 eV and select I: region of 1 or more of the small pipa particles. Save as *-PIPA.

8.	select a region  with no particles – save as *-matrix.

#### D.3 Creating chemical maps from SVD fits

9. 	Stacks~maps~SVD  - select *od.ncb

10.	define 3 components – select the *-matrix, *-PIPA  and *-SAN

as the reference spectra; save as matrix-pipa-SAN-14od.par

11.	the Singular value decomposition fit will then execute, displaying the 3 reference spectra in buffers 1-3, and the 3 component maps in buffers 4-6, and the residual (data – fit) averaged over all photon energies in buffer 9.

12.	Images~clip~histogram each of the component maps to remove –ve tails to improve contrast

12. Display~RBG composite (buffers 4, 5, 6) to make color composite of the 3 components. Select ‘Yes’ to rescale within  each color